## Slide 1
Approximated losses from ZnS data (2mm thick, normal incidence)
since transmittance increases with wavelength, im(n) needs to decrease in this region
try form k(λ) = m(λ – 2[um]) + b (m < 0 , b > 0)
Find ‘m’ and ‘b‘ empirically to match transmittance data

## Slide 2
Approximated losses from ZnS data
k(λ) = m(λ – 2[um]) + b , with
m = -3 x 10-7 and b = 1.5 x 10-6
Ignore feature close to 2 microns

## Slide 3
…
…
thicknesses (μm)
[300, 0.1, 0.02, 0.1, 0.2]
nZnS
nZnS
nSi
nC
nSiO2
@ λ = 2.8μm:
nZnS = 2.25
nSi = 3.56
nC = 4.53 + 3.64i
nSiO2 = 1.42
Adding losses to 300μm bulk yields 0.1% change in transmittance
Final design: