## Slide 1: How can a spatial Kramers–Kronig coating help?
window
coating
Rf (signal)
I0
T
Rb (noise)
1. Coating behind window (e.g. ellipsometry)
window
coating
I0
T0
2. Coating in front of window (e.g. TE detection)
FOM:
Tf
εb (noise)
εL
εR (noise)
εW (noise)
FOM:

## Slide 2: Plan and Intuition
Use different portions of KK profile for coating
Compare FOM of sKK coating and AR coating
Intuition: sKK coating will not help (trading reflection for emission, not transmission)

## Slide 3
I0
noise = RLR
noise=0.071
noise=0.58
noise=0.63
1. Ellipsometry (Bare Window)

## Slide 4
noise = RLR + EL
EL = ALR
RLR=0.071, ALR=0, noise=0.071
RLR=0.057, ALR=0.056, noise=0.11
semi-infinite layer on left is the bulk material, which is assumed to be max value of real part of dielectric function.
semi-infinite layer on the right is air.
adding losses lowers reflectance, but adds emission, so more noise overall.
adding dispersion will likely not change results (still trading reflection for emission).
I0
Wavelength dependence

## Slide 5
RLR=0.59, ALR=0, noise=0.59
RLR=0.51, ALR=0.1, noise=0.61
adding losses does not help (trading reflection for emission, which is still noise).
RLR=0.48, ALR=0.086, noise=0.57
RLR=0.54, ALR=0, noise=0.54
noise = RLR + EL
EL = ALR
I0
Angle dependence

## Slide 6
T=0.72, ARL=0.17, FOM=4.29
T=0.69, ARL=0.21, FOM=3.33
window is 5mm sapphire with k = 10-5
adding losses lowers transmission and increases emission (no benefit)
signal = T
noise = ER = ARL
FOM = signal / noise
Wavelength dependence
I0

## Slide 7
Same conclusion for angle dependence: FOM gets worse for sKK coating for both s and p polarizations.
T=0.57, ARL=0.18, FOM=3.15
T=0.54, ARL=0.23, FOM=2.4
T=0.69, ARL=0.24, FOM=2.85
T=0.73, ARL=0.2, FOM=3.7
signal = T
noise = ER = ARL
FOM = signal / noise
Angle dependence
I0

## Slide 8
noise = RLR + ALR
noise = 0.055
noise = 0.115
semi-infinite layer on left is window, which is assumed to be max value of real part of dielectric function.
semi-infinite layer on the right is min value of Re(eps).
assumed that materials between n=1 and n=1.4 exist, to show whether adding losses help or not.
I0