## Slide 1
Hilbert Transform: Why Symmetric Endpoints Matter
Left: Lorentzian profile has same endpoints — FFT-based HT works perfectly. Right: GRIN coating has different endpoints. FFT assumes periodicity → jump discontinuity → the root cause of unwanted artifacts.

## Slide 2
The Hilbert Transform Problem: Asymmetric Endpoints
sKK requires computing ε'' = H[ε']. For coatings on substrates, ε'(−∞) = εb ≠ 1 = ε'(+∞). FFT-based HT assumes periodicity → endpoint mismatch causes gain regions.

## Slide 3
Derivative-then-Integrate: Solving the Endpoint Problem
Take derivative of ε'(x) → both endpoints go to 0 → standard HT works → integrate back. Result: well-localized ε'' peak, but "lossy air" region (n ≈ 1, k > 0) persists — this is fundamental to the asymmetric HT.

## Slide 4
Backside Reflection Reduction: sKK vs GRIN vs Bulk
s-pol, 80°: sKK coating reduces ⟨Rback⟩ from 0.129 (bulk) to 0.022, a >5× improvement. GRIN alone provides negligible benefit (0.128) at this sub-λ thickness.

## Slide 5
Angle-Dependence of Backside Reflection at λ = 3 μm
sKK coating reduces backside reflection at all angles for both polarizations. Performance particularly strong at ellipsometric angles (60–80°).

## Slide 6
Quantifying Analyticity: Spectral One-Sidedness
1. Form complex derivative function:
z(x) = dε′/dx + i · dε′′/dx
2. Fourier transform to spatial frequency:
Z(k) = FFT{ z(x) } (k = spatial wavenumber (μm⁻¹))
3. Measure one-sidedness:
E₊ = ∫ |Z(k)|² dk for k > 0
E₋ = ∫ |Z(k)|² dk for k < 0
FoM = 100 * (E₊ − E₋) / (E₊ + E₋)
Physical meaning: sKK requires ε(x) analytic in upper half-plane → its spatial spectrum is one-sided. Positive k = no reflection from one direction.

## Slide 7
Quantifying Analyticity: Spectral One-Sidedness
check FoM function with complex Lorentzian:

## Slide 8
R → A Trade-off: Sweeping Loss Magnitude
ε''mod = α · ε''sKK
R, A averaged over 2–5 μm.
Crossing point at α ≈ 0.12:
⟨R⟩ = ⟨A⟩ ≈ 0.10
α = 0 (GRIN only):
⟨R⟩ = 0.128, FoM = 0%
α = 1 (full sKK):
⟨R⟩ = 0.022, FoM = 96.4%
Reducing α lowers absorption but also destroys analyticity (purple dashed).

## Slide 9
Smooth Gating Removes Unphysical "Lossy Air" Region

## Slide 10
Analyticity Cost: Full sKK vs Gated Profile
Full sKK (left): nearly all spectral weight on positive k → FoM = 96.4%. Gated σ = 0.1 (right): removing lossy air injects power into forbidden (negative k) side → FoM drops to 17.5%. Every practical mitigation breaks analyticity.

## Slide 11
Design Space: GRIN vs sKK Across Coating Thickness
Three regimes: Sub-λ coatings (<1.5 μm) where GRIN is ineffective and sKK provides the only path to low R — but at the cost of absorption and broken analyticity. Thick coatings (>6 μm) where GRIN alone achieves low R without absorption. Crossover region (1.5–6 μm) is where the design tradeoff is most nuanced.
averaged Rback between 2-5um (s-pol, 80deg):

## Slide 12
Paper Plan
The Problem
Computing the Hilbert transform of GRIN profiles with asymmetric endpoints (ε′(−∞) ≠ ε′(+∞)) is essential for coating application of sKK, and the standard FFT-based HT fails due to periodic continuation artifacts.
The Method
Derivative-then-integrate: dε′/dx → 0 at both endpoints, so the standard HT works on the derivative. Integrate back to recover ε′′.
Results
Achieve zero-reflectance for all angles and wavelengths but with “lossy air” (n ≈ 1, k > 0), which is fundamental to the asymmetric HT — not a numerical artifact (Horsley et al. perfect transmission via gain). First quantitative characterization of the analyticity–physicality tradeoff using spectral one-sidedness FoM.
Three thickness regimes: sub-λ (sKK essential, GRIN ineffective), crossover (1.5–6 μm), and thick coatings (>6 μm, GRIN alone suffices).
Practical mitigations (α-scaling, σ-gating) trade practicality for reflection reduction and broken analyticity.