## Slide 1: How can a spatial Kramers–Kronig coating help?
window
coating
Rf (signal)
I0
T
Rb (noise)
1. Coating behind window (e.g. ellipsometry)
window
coating
I0
2. Coating in front of window (e.g. TE detection)
FOM:
T
εb (noise)
ε (noise)
FOM:

## Slide 2: Plan and Intuition
Use different portions of KK profile for coating
Compare FOM of sKK coating and AR coating
Intuition: sKK coating will not help (trading reflection for absorption, not transmission)

## Slide 3
Optical Response of 5mm Bulk Sapphire

## Slide 4
Optical Response of 5mm Bulk Sapphire (Angle Dependence)

## Slide 5
noise = Rb + Ab
Rb=0.05, Ab=0.05, noise=0.1
1. With x0=0.01um s-KK Coating (ellipsometry)
Rb=0.04, Ab=0.1, noise=0.14
coating slightly decreases Rb but increases Eb, causing overall noise to increase

## Slide 6
noise = Rb + Eb
Rb=0.05, Eb=0.05, noise=0.1
1. With x0=1um, 10% Im(n) s-KK Coating
Rb=0, Eb=0.37, noise=0.37
thicker coating layers eliminate Rb but increase Eb significantly, even when 10% Im(n) used

## Slide 7
noise = Rb + Eb
Rb=0.05, Eb=0.05, noise=0.1
1. With x0=1um, 1% Im(n) s-KK Coating
Rb=0, Eb=0.087, noise=0.087
with 1% Im(n), noise is lower, showing that traditional GRIN coating is better than coating with losses

## Slide 8
noise = Rb + Eb
Rb=0.03, Eb=0.38, noise=0.41
1. Angle Dependence With x0=0.01um s-KK Coating
Rb=0.027, Eb=0.4, noise=0.42
similar to wavelength dependence: coating slightly decreases Rb but increases Eb

## Slide 9
noise = Rb + Eb
1. With x0=1um, 10% Im(n) s-KK Coating
Rb=0.003, Eb=0.5, noise=0.5
same story: thicker coating layers eliminate Rb but increase Eb
Rb=0.03, Eb=0.38, noise=0.41

## Slide 10
noise = Rb + Eb
1. With x0=1um, 1% Im(n) s-KK Coating
Rb=0.005, Eb=0.38, noise=0.38
same conclusion: losses do not help with this problem
Rb=0.03, Eb=0.38, noise=0.41

## Slide 11
FOM = Tavg / Eavg
Tavg=0.83, Eavg=0.05, FOM=16.8
2. With x0=0.01um s-KK Coating (TE)
coating decreases transmission and increases emission (opposite of what we want)
Tavg=0.68, Eavg=0.21, FOM=3.22