## Slide 1
Hilbert Transform: Why Symmetric Endpoints Matter
Left: Lorentzian profile has same endpoints — FFT-based HT works perfectly. Right: GRIN coating has different endpoints. FFT assumes periodicity → jump discontinuity → the root cause of unwanted artifacts.

## Slide 2
The Hilbert Transform Problem: Asymmetric Endpoints
sKK requires computing ε'' = H[ε']. For coatings on substrates, ε'(−∞) = εb ≠ 1 = ε'(+∞). FFT-based HT assumes periodicity → endpoint mismatch causes gain regions.

## Slide 3
Derivative-then-Integrate: Solving the Endpoint Problem
Take derivative of ε'(x) → both endpoints go to 0 → standard HT works → integrate back. Result: well-localized ε'' peak, but "lossy air" region (n ≈ 1, k > 0) persists — this is fundamental to the asymmetric HT.

## Slide 4
Backside Reflection Reduction: sKK vs GRIN vs Bulk
s-pol, 80°: sKK coating reduces ⟨Rback⟩ from 0.129 (bulk) to 0.022, a >5× improvement. GRIN alone provides negligible benefit (0.128) at this sub-λ thickness.

## Slide 5
Angle-Dependence of Backside Reflection at λ = 3 μm
sKK coating reduces backside reflection at all angles for both polarizations. Performance particularly strong at ellipsometric angles (60–80°).

## Slide 6
Quantifying Analyticity: Spectral One-Sidedness
1. Form complex derivative function:
z(x) = dε′/dx + i · dε′′/dx
2. Fourier transform to spatial frequency:
Z(k) = FFT{ z(x) } (k = spatial wavenumber (μm⁻¹))
3. Measure one-sidedness:
E₊ = ∫ |Z(k)|² dk for k > 0
E₋ = ∫ |Z(k)|² dk for k < 0
FoM = 100 * (E₊ − E₋) / (E₊ + E₋)
Physical meaning: sKK requires ε(x) analytic in upper half-plane → its spatial spectrum is one-sided. Positive k = no reflection from one direction.

## Slide 7
spatial frequency k is the fourier conjugate of position x. low k means slowly varying features

## Slide 8
Quantifying Analyticity: Spectral One-Sidedness
check FoM function with complex Lorentzian:

## Slide 9
R → A Trade-off: Sweeping Loss Magnitude
ε''mod = α · ε''sKK
R, A averaged over 2–5 μm.
Crossing point at α ≈ 0.12:
⟨R⟩ = ⟨A⟩ ≈ 0.10
α = 0 (GRIN only):
⟨R⟩ = 0.128, FoM = 0%
α = 1 (full sKK):
⟨R⟩ = 0.022, FoM = 96.4%
Reducing α lowers absorption but also destroys analyticity (purple dashed).

## Slide 10
Smooth Gating Removes Unphysical "Lossy Air" Region

## Slide 11
Analyticity Cost: Full sKK vs Gated Profile
Full sKK (left): nearly all spectral weight on positive k → FoM = 96.4%. Gated σ = 0.1 (right): removing lossy air injects power into forbidden (negative k) side → FoM drops to 17.5%. Every practical mitigation breaks analyticity.

## Slide 12
Hold Total Losses Constant, Vary Loss Shape (s-pol, 80°)
constant profile performs slightly worse than sKK profile

## Slide 13
Hold Total Losses Constant, Vary Loss Shape (s-pol, 80°)
both double peaks and random distribution perform slightly worse than sKK profile

## Slide 14
Hold Total Losses Constant, Vary Loss Shape (s-pol, 80°)
gaussian performs slightly better than sKK with lower FoM

## Slide 15
Hold Total Losses Constant, Vary Loss Shape (s-pol, 80°, gated)
for gated profiles, constant again performs slightly worse than sKK gated

## Slide 16
Hold Total Losses Constant, Vary Loss Shape (s-pol, 80°, gated)
both double peaks and random distribution perform slightly worse than sKK gated

## Slide 17
Hold Total Losses Constant, Vary Loss Shape (s-pol, 80°, gated)
again, gaussian performs better than sKK. could be the smoother increase in imaginary part.

## Slide 18
Repeat Experiment with 10x Coating Thickness (s-pol, 80°)
sKK shape outperforms other shapes at 4um thickness, but not at 0.4um
my guess: sKK is a coherent effect, which requires phase to accumulate within each layer. if layers are much smaller than the incoming wavelength (2-5um), there is no phase accumulation or cancellation, so only the total loss matters (not the shape). thicker layers allow for sKK to do its thing, while accumulating reflections for other non-HT profiles.

## Slide 20
Design Space: GRIN vs sKK Across Coating Thickness
Three regimes: Sub-λ coatings (<1.5 μm) where GRIN is ineffective and sKK provides the only path to low R — but at the cost of absorption and broken analyticity. Thick coatings (>6 μm) where GRIN alone achieves low R without absorption. Crossover region (1.5–6 μm) is where the design tradeoff is most nuanced.
averaged Rback between 2-5um (s-pol, 80deg):

## Slide 21
Paper Plan
The Problem
Computing the Hilbert transform of GRIN profiles with asymmetric endpoints (ε′(−∞) ≠ ε′(+∞)) is essential for coating application of sKK, and the standard FFT-based HT fails due to periodic continuation artifacts.
The Method
Derivative-then-integrate: dε′/dx → 0 at both endpoints, so the standard HT works on the derivative. Integrate back to recover ε′′.
Results
Achieve zero-reflectance for all angles and wavelengths but with “lossy air” (n ≈ 1, k > 0), which is fundamental to the asymmetric HT — not a numerical artifact (Horsley et al. perfect transmission via gain). First quantitative characterization of the analyticity–physicality tradeoff using spectral one-sidedness FoM.
Three thickness regimes: sub-λ (sKK essential, GRIN ineffective), crossover (1.5–6 μm), and thick coatings (>6 μm, GRIN alone suffices).
Practical mitigations (α-scaling, σ-gating) trade practicality for reflection reduction and broken analyticity.